# Product Data Sheet

Page 1 of 2

HIGH SOLIDS RED EPOXY PRIMER

| CHARACTERISTICS Product Description: This product is a high solids, two component, low VOC (2.1 lbs/gal) polyamide primer. Resulting in a highly corrosion resistant coating. The primer has excellent adhesion over properly prepared cold rolled steel. Suggested uses: High build primer up to 5 mils DFT over abrasive blasted cold rolled steel where topcoat is required. No induction time and long pot life improves productivity. Spray application with minimal dry overspray. Not recommended for immersion service. Intended to be used as a primer and should be top coated. Compatibility with other coatings. Aexcel high solids epoxy is compatible with most coating types in good condition. Test should be performed to assure adhesion and compatibility in an inconspicuous place before work begins. Weight Solids activated: 70.5 ± 2% Volume Solids activated: 53.3 ± 2% Weight/Gallon Part A: 12.93 ± .20 lbs. Weight/Gallon Catalyzed system: 11.90 ± .20 lbs. VOC/Gallon Part A: 2.3 lbs /gal, 283g/L VOC/Gallon activated system: 2.09 lbs /gal, 251g/L Flash Point: 40 °F. Gloss @ 60: 15.0 @ 3 mills. Higher film thickness brings higher gloss. Coverage Rate: 855 sq./ft. per gal. @ 1mill dry film thickness. 285 sq./ft. per gal. @ 3mills dry film thickness. 171 sq./ft. per gal. @ 5mills dry film thickness. Cure time- hours: 77°F 50% RH 3 mill drawdown. Dry to touch. 3-4 hours Dry hard. 8 hours Pot life. 4 hours Dry to top coat. 15 hours *Temperature, relative humidity, and film thickness will affect dry time. APPLICATION Substrate: Cold rolled steel. Surface Preparation: Commercial blasting SSPC-SP-6 will provide very good performance. If not possible Hand Tool clean SSPC-SP2 or Power Tool clean SSPC-SP-3 is acceptable with some sacrifice in performance vs blasting. Sanding and phosphating is acceptable as long as the surface is clean, dry, free from dust, chemicals and other contamination. Surface profile must be 1.5 to 2.5 mils average peak to valley. Activation: Using a shear mixer mix each component thoroughly at low speed before combining. At low speed create a small vortex and add the activator. Continue mixing until a thoroughly blended. Painting may begin immediately. No induction time is needed. Reduction: Reduction is not needed for spray application. May be brushed or rolled with some sacrifice in appearance. *Material losses during mixing and application will vary and must be taken into consideration when estimating material quantities needed to complete a project. *High humidity 90% should be avoided during initial application and drying. High humidity may cause blushing or a microscopic layer of moisture on the surface which can cause adhesion problems between the primer and top coat. | PERFORMANCE PROPERTIES: Primer only Adhesion by tape test per ASTM D 3359-90 Rating: 4B Sag ASTM D4400-889 12 mills Pencil Hardness ASTM D3363-72 2H Salt Fog per ASTM B-117 1,000 hours Creep at scribe Rating: 9-10, 0 to 1/64 inch Blister at scribe Rating: 9-10 few small to none Blister un-scribed area Rating: 10 none Ratings are 0=very poor to 10=Excellent PERFORMANCE PROPERTIES: With Aexcel High Performance 2K Polyurethane Topcoat. Acids- Very Good Alkalis- Excellent Solvents- Excellent Weathering- Excellent (will chalk if not top coated) Humidity- Excellent Storage: Store at room temperature. KEEP FROM FREEZING Aexcel high solids epoxy may settle. Mix each component thoroughly using a shear mixer at low speed before activating. APPLICATION Substrate: Cold rolled steel. Surface Preparation: Commercial blasting SSPC-SP-6 will provide very good performance. If not possible Hand Tool clean SSPC-SP2 or Power Tool clean SSPC-SP-3 is acceptable with some sacrifice in performance vs blasting. Sanding and phosphating is acceptable as long as the surface is clean, dry, free from dust, chemicals and other contamination. Surface profile must be 1.5 to 2.5 mils average peak to valley. Activation: Using a shear mixer mix each component thoroughly at low speed before combining. At low speed create a small vortex and add the activator. Continue mixing until a thoroughly blended. Painting may begin immediately. No induction time is needed. Reduction: Reduction is not needed for spray application. May be brushed or rolled with some sacrifice in appearance. *Material losses during mixing and application will vary and must be taken into consideration. *High humidity 90% should be avoided during initial application and drying. High humidity may cause blushing or a microscopic layer of moisture on the surface which can cause adhesion problems between the primer and top coat. SUGGESTED FILM BUILD: 6 mils (150 µm) wet 3 mils (75 µm) dry Equipment: Spray application 2001 BINKS Fluid Nozzle- 63CSS Air Cap- 63PR Others may be used. Changes in pressure and tip size may be required. Roll & Brush: ¼ - ½ inch Nap Roller cover. Keep roller wet. Roll in one direction, rewet, then cross roll. Brush apply with china bristle brush. Clean Up: After shutdown or before a long delay, PROMPT CLEAN UP OF ALL EQUIPMENT IS ESSENTIAL, IF EQUIPMENT DAMAGE IS TO BE AVOIDED. This applies to pots, lines, hoses and guns. Use Acetone or Xylene wash thinners. |
| --- | --- |

Aexcel Corporation • 7373 Production Drive • Mentor, Ohio  44060 • Phone: 440-974-3800 • Fax: 440-974-3808

The Product data offered herein are, to the best of our knowledge, true and accurate, but all recommendations are made without warranty, express or implied.  Since the conditions of use are beyond our control, neither Aexcel Corporation, nor its agents shall be liable for any injury, loss or damage, direct or consequential, arising from the use or the inability to use the product described herein.  No person is authorized to make any statement or recommendation not contained in the Product Data, and any such statement or recommendation, if made, shall not bind the Corporation.  Further, nothing contained herein shall be construed as a recommendation to use any product in conflict with existing patents, and no license under the claims of any patent is either implied or granted.