# Product Data Sheet

55W-J043 White High Performance 2K UTHANE® Topcoat

| # CHARACTERISTICS Product Description: This product is a two-component, high solids, low VOC, acrylic polyurethane. It is designed for high performance protection with outstanding exterior gloss and color retention. Suggested uses: High performance topcoat for use as DTM or over 45R-H001 2K Red Epoxy Primer for enhanced protection of exterior storage tanks. Compatibility with other coatings. Aexcel high solids polyurethane is compatible with most coating types in good condition. Testing should be performed to assure adhesion and compatibility in an inconspicuous place before work begins. Wt. Solids Activated: 69.8 ± 2% Vol. Solids Activated: 57.2 ± 2% Wt./gl. Part A: 10.83 ± .2 lbs. VOC: Part A: 3.82 lb./gl. 458 g/l VOC: Activated system: 3.26 lb./gl. 391g/l Flash Point: 77 °F. Gloss @ 60: 90.0 @ 3 mils DFT. Coverage Rate: 916 sq. /ft. per gl. @ 1mils DFT. 305 sq. /ft. per gl. @ 3 mils DFT. 183 sq. /ft. per gl. @ 5 mils DFT. | # APPLICATION Surface Preparation: For Direct to Metal application substrate must be clean and free of contamination. Newly primed surface should be clean and dry. Previously painted surfaces should have all loose paint removed and edges feathered. Prime bare spots with 45R-H001 2K Red Epoxy Primer. Activation: Thoroughly mix 6 parts 55W-J043 White HP Polyurethane with 1 part of 95C-F063 Activator. Mix each component Reduction: No reduction required. Potlife: 3 hours @ 77 °F. (Activated) Equipment: Mix by hand or 2 component proportion pump Cure time- hours: *77°F @ 50% RH - 3 mil drawdown. Dry to Touch: 4 hrs. Dry to Recoat: 4 hrs. Dry to Handle: 8 hrs. Pack / Ship: 24 hrs. Full Cure: 7 Days *Temperature, relative humidity, and film thickness will affect dry time. SUGGESTED FILM BUILD: 6 mils (150 µm) wet 3 mils (75 µm) dry Wash Thinner: Ketones are most effective. Do not use aliphatics or alcohols. |
| --- | --- |

Uthane is a registered trademark of Aexcel Corporation, all rights reserved.

## Aexcel Corporation    7373 Production Drive    Mentor, Ohio  44060    Phone: 440-974-3800    Fax: 440-974-3808

The Product data offered herein are, to the best of our knowledge, true and accurate, but all recommendations are made without warranty, express or implied.  Since the conditions of use are beyond our control, neither Aexcel Corporation, nor its agents shall be liable for any injury, loss or damage, direct or consequential, arising from the use or the inability to use the product described herein.  No person is authorized to make any statement or recommendation not contained in the Product Data, and any such statement or recommendation, if made, shall not bind the Corporation.  Further, nothing contained herein shall be construed as a recommendation to use any product in conflict with existing patents, and no license under the claims of any patent is either implied or granted.

55W-J043 White High Performance 2K UTHANE® Topcoat

| Equipment: Spray application: 2001 BINKS Fluid Nozzle- 63CSS Air Cap- 63PR Others may be used. Changes in pressure and tip size may be required. Roll & Brush: ¼ - ½ inch Nap Roller cover. Keep roller wet. Roll in one direction, rewet, then cross roll. Brush apply with china bristle brush. Do not cross brush to reduce lap marks. Clean Up: After shutdown or before a long delay, PROMPT CLEAN UP OF ALL EQUIPMENT IS ESSENTIAL, IF EQUIPMENT DAMAGE IS TO BE AVOIDED. This applies to pots, lines, hoses and guns. Use MEK, Acetone, or Xylene wash thinners Performance Properties: When applied over 45R-___High Solids 2K Red Epoxy Primer. Adhesion: by tape test ASTM D 3359-90 Rating: 4B Sag: ASTM D4400-889 8.0 mills Salt Fog: ASTM B-117 1,000 hours Creep No Scribe: Rating: 10 None Blistering No Scribe: Rating: 10 None Ratings: 0 -10 =Very poor - 10 = Excellent Humidity Resistance: ASTM D2247 1,000 hours No Rusting No Blistering Gloss: ASTM D4587 8 hrs. UV @ 50° C, 4 hrs. condensation @ 40° C. Initial gloss @ 60° = 95 3,000 hrs. QUV A gloss @ 60° = 92 CHEMICAL RESISTANCE: The following chemicals had no effect (24 hours watch glass) 10% Sulfuric Acid 10% Hydrochloric Acid 10% Acetic Acid 50% Sodium Hydroxide 30% Ammonium Hydroxide Distilled Water MEK Toluene Methanol Isopropanol Unleaded Gasoline | All polyurethane systems, whether single or multi-component, are sensitive to moisture and will gel or begin to cure if permitted to come into contact with humid air or water. This includes the exposure of the coating in open containers or contact with moisture in fluid and air lines. Air compressors should be equipped with moisture traps, driers, and filters to ensure that the coating does not "see" moist air. In this way, damage to equipment can be avoided. # PRECAUTIONS Safe Handling: When this product has been combined with our urethane curing agent, aliphatic and/or aromatic polyisocyanates then are present, which give off harmful vapors of isocyanates (hazardous materials) when sprayed. Do not use if you have chronic (long-term) lung or breathing problems, or if you have ever had a reaction to isocyanates. Use only with adequate ventilation. Where overspray is present, a positive-pressure, air-supplied respirator (TC-19C NIOSH/MESA) is recommended. If not available, use a vapor/particulate respirator that respirator supplier recommends as effective for isocyanate vapors and mists, such as a NIOSH TC-23C type. Refer to our Data Sheet "Safety in the Handling and Use of Uthanes," and to the Material Safety Data Sheet, available upon request. First Aid: If affected by inhalation of vapor or spray mist, remove to fresh air. If breathing difficulty persists or occurs later, consult a physician and have label information available. In case of eye contact, flush immediately with plenty of water for 15 minutes; call a physician. In case of skin contact, wash thoroughly with soap and water. |
| --- | --- |

## Aexcel Corporation    7373 Production Drive    Mentor, Ohio  44060    Phone: 440-974-3800    Fax: 440-974-3808

The Product data offered herein are, to the best of our knowledge, true and accurate, but all recommendations are made without warranty, express or implied.  Since the conditions of use are beyond our control, neither Aexcel Corporation, nor its agents shall be liable for any injury, loss or damage, direct or consequential, arising from the use or the inability to use the product described herein.  No person is authorized to make any statement or recommendation not contained in the Product Data, and any such statement or recommendation, if made, shall not bind the Corporation.  Further, nothing contained herein shall be construed as a recommendation to use any product in conflict with existing patents, and no license under the claims of any patent is either implied or granted.