95C-F005 UTHANE® EXTERIOR CURING AGENT

(4/22/96 (Supersedes 2/20/96)

| # CHARACTERISTICS Product Description: A premium aliphatic urethane adduct. It is used in exempt low free monomer ASTM Type II-B two-component urethanes. Weight Solids: 75.0 ± 2% Volume Solids: 70.0 ± 2% Weight/Gallon: 8.9 lbs. Flash Point: 87°F (DOT red label) Free Isocyanate: Less than .7% free monomer (w/w resin solids) Storage: Normal--avoid heat, water, moisture, and exposure to the atmosphere. ®Uthane is a registered trademark of Aexcel Corporation, rights reserved. | # APPLICATION Cleaning Solvent: n-Butyl Acetate, Xylol. Do not use water, alcohols, or amines. PRECAUTIONS Safe Handling: Contains aliphatic and/or aromatic polyisocyanates, which give off harmful vapors of isocyanates (hazardous materials). Do not use if you have chronic (long-term) lung or breathing problems, or if you have ever had a reaction to isocyanates. Use only with adequate ventilation. Where overspray is present, a positive-pressure, air-supplied respirator (TC-19C NIOSH/ MESA) is recommended. If not available, use a vapor/ particulate respirator that respirator supplier recommends as effective for isocyanate vapors and mists, such as a NIOSH TC-23C type. Refer to our Data Sheet "Safety in the Handling and Use of Uthanes," and to the Material Safety Data Sheet, available upon request. First Aid: If affected by inhalation of vapor or spray mist, remove to fresh air. If breathing difficulty persists or occurs later, consult a physician and have label information available. In case of eye contact, flush immediately with plenty of water for 15 minutes; call a physician. In case of skin contact, wash thoroughly with soap and water. |
| --- | --- |